The selected flooring similar to Omnisports Reference Multi-use must comply with EN 14 904 standard requirements and is classified P1, available in 2m wide roll.

The product formulation does not contain phthalate-based plasticizer. It is built on a calendared backing layer made of recycled vinyl flooring material. It contains over 21% recycled material.

The sports vinyl floor covering is reinforced with a non-woven fiber glass mat combined with a high density closed-cell foam. The foam backing must be deeply embossed to reinforce the suction effect.

The wear layer is reinforced with UV photo-crosslinked polyurethane Top Clean XP™ applied in factory. The product must offer the same top embossing between solid and wood designs.

The total thickness should be at least equal to 6.2mm.

The product should offer resistance to static indentation lower than 0.10mm and vertical deformation lower than 2mm. It should offer ball rebound at least equal to 95%.

It offers a dimensional stability lower than 0.10% according to EN ISO 23999. The resistance to wear should be <0.2g according to EN ISO 5470-1.

The fire resistance according to EN13501-1 should be at least Cfl-s1.

The product must not trigger any disease related to asthma and allergy and should be covered by the Seal of Approval delivered by Allergy UK standard.

Its emission rate of volatile organic compounds in air is very low, measured after 28 days according to EN standard 16516. Close to zero emission (quantification limit), TVOC, TSVOC and formaldehyde emissions are below 10 µg/m3.

In alignment with the goal of eliminating substances that may have adverse effects on users’ health and the environment, biocide-free products should be prioritized.

The product should be 100% recyclable. The clean off-cuts can be collected, recycled and reused in the production of vinyl floor coverings through Restart® program or similar.

The selected flooring is covered by a specific third-party verified Environmental Product Declaration (EPD), disclosing among other indicators the carbon footprint of the flooring during its whole lifecycle.

The selected flooring is covered by a third-party verified ingredient disclosure and material risk declaration down to 0.01%w, thus ensuring compliance far beyond REACH regulation requirements, such as Material Health Statement (MHS).

Product warranty should be equal or superior to 15 years.

The installation of the vinyl sports flooring can be implemented using perimeter glue method – minimum 90% adhesive-free, on a subfloor with humidity rate up to 7%. Above this rate the subfloor is considered saturated. (See the manufacturer’s installation guide)

The product should be recommended by the international federations of Basketball - FIBA

Available documentation & certificates

- Technical datasheet

- Multi-language DoP (Declaration of Performance)

- EN 14904 certificate of compliance

- Reaction to fire test report

- Dimensional stability certificate (internal)

- Wear layer thickness certificate (internal)

- Acoustic efficiency report EN ISO 717-2

- Thermal resistance EN ISO 10456

- Installation and maintenance guides

- FIBA certificate

Environmental certificates

- Tarkett Indoor Air Quality certificate

- Eurofins VOC emissions report

- Allergy UK Seal of Approval

- MHS – Material Health Statement

- EPD – Environmental Product Declaration

Contact us

For any additional information, Tarkett Sports experts remain at your disposal to assist you throughout your project.

info.tarkettsports.indoor@tarkett.com
 eu.tarkettsportsindoor.com